TÓM TẮT THÔNG TIN VỀ LUẬN ÁN

Tên đề tài luận án: Nghiên cứu và phát triển phương pháp đo độ dày của tấm vật liệu dựa trên kỹ thuật gamma truyền qua

Ngành: Vật lý nguyên tử và hạt nhân

Mã số ngành: 62440501

Họ tên nghiên cứu sinh: Huỳnh Đình Chương

Khóa đào tạo: 2016

Người hướng dẫn khoa học: PGS.TS. Trần Thiện Thanh

Cơ sở đào tạo: Trường Đại học Khoa học Tự nhiên, ĐHQG-HCM

1. TÓM TẮT NỘI DUNG LUẬN ÁN:

Luận án tập trung phát triển hệ đo gamma truyền qua (GT) sử dụng nguồn phóng xạ 137Cs và đầu dò NaI(Tl) để xác định độ dày của các tấm vật liệu đồng nhất. Chương trình MCNP phiên bản 6.1 được ứng dụng để mô phỏng các phép đo gamma truyền qua, nhằm tạo ra cơ sở dữ liệu phục vụ cho việc hiệu chuẩn hệ đo. Để đảm bảo độ chính xác cao của các kết quả mô phỏng, cấu hình mô phỏng của đầu dò NaI(Tl) được xây dựng dựa trên các thông số kỹ thuật thu được từ phương pháp quét chùm photon năng lượng thấp. Kết quả cho thấy hiệu suất đỉnh năng lượng toàn phần tính được từ mô phỏng có sự phù hợp tốt so với giá trị thực nghiệm. Cụ thể, độ khác biệt tương đối (RD) nhỏ hơn 3,5 % trong khoảng năng lượng 31 – 1408 keV, cho các phép đo nguồn chuẩn tại khoảng cách 0 mm và 300 mm.

Dựa trên mô phỏng, luận án đã xây dựng một bộ dữ liệu phổ GT đa dạng, tương ứng với các vật liệu có số nguyên tử hiệu dụng từ 3 đến 83 và độ dày mẫu trong khoảng từ 0,1 mm đến 70 mm. Một đại lượng gọi là tỉ số R được tính bằng cách lấy diện tích đỉnh của phép đo có mẫu chia cho phép đo không có mẫu. Các giá trị của ln(R) mô phỏng được sử dụng để xây dựng đường chuẩn phân tích cho việc xác định độ dày. Độ dày của một mẫu thực tế được suy ra bằng cách nội suy giá trị của ln(R) thực nghiệm vào trong đường chuẩn phân tích. Độ chính xác của phương pháp đề xuất được kiểm chứng thông qua dữ liệu từ 162 phép đo thực nghiệm trên các mẫu graphit, nhôm, thép C45 và đồng. Kết quả cho thấy RD trung bình giữa độ dày đo được và độ dày thực tế là 0,52%, trong khi RD lớn nhất là 2,17%.

Ngoài ra, luận án cũng phát triển một phương pháp ước tính khoảng độ dày đo được (RMT) tương ứng với các độ chính xác mong muốn (DA) trong kỹ thuật GT. Kết quả cho thấy, với mọi phép đo mà độ dày của mẫu nằm trong RMT, giá trị của RD luôn nhỏ hơn giá trị DA đặt ra.

2. NHỮNG KẾT QUẢ MỚI CỦA LUẬN ÁN:

- Đề xuất phương pháp quét chùm photon năng lượng thấp nhằm xác định các thông số kỹ thuật quan trọng của đầu dò NaI(Tl), bao gồm đường kính và chiều dài tinh thể, khoảng cách từ cửa sổ đến tinh thể và mật độ khối lượng của lớp phản xạ. Những thông số này được sử dụng để xây dựng cấu hình mô phỏng, giúp tạo ra dữ liệu mô phỏng với độ chính xác cao.

- Đề xuất công thức làm khớp cho phép tính toán nhanh và chính xác hệ số tích lũy (buildup factor), áp dụng hiệu quả cho các vật liệu có số nguyên tử hiệu dụng trong khoảng từ 3 đến 83 và độ dày mẫu nhỏ hơn 70 mm. Công thức này giúp đánh giá sự đóng góp của các gamma tán xạ trong kỹ thuật GT.

- Đề xuất phương pháp bán thực nghiệm để xác định độ dày của tấm vật liệu dựa trên phổ đo được từ kỹ thuật GT, trong đó đường chuẩn phân tích được xây dựng hoàn toàn từ dữ liệu mô phỏng. Phương pháp này giúp giảm chi phí vận hành và tăng tính linh hoạt của thiết bị trong các ứng dụng thực tế, đặc biệt phù hợp khi đo độ dày cho nhiều loại vật liệu khác nhau.

- Đề xuất phương pháp ước tính khoảng độ dày có thể đo được với độ chính xác mong muốn trong kỹ thuật GT. Phương pháp này hỗ trợ người sử dụng chủ động lựa chọn tham số đo phù hợp, tối ưu hóa cấu hình đo và thời gian đo, đồng thời đảm bảo độ tin cậy của kết quả trong các ứng dụng kiểm tra không phá hủy.

3. CÁC ỨNG DỤNG/ KHẢ NĂNG ỨNG DỤNG TRONG THỰC TIỄN HAY NHỮNG VẤN ĐỀ CÒN BỎ NGỎ CẦN TIẾP TỤC NGHIÊN CỨU

Các kết quả nghiên cứu của luận án có khả năng ứng dụng trực tiếp vào việc kiểm tra độ dày của các tấm vật liệu trên dây chuyền sản xuất công nghiệp, nhằm đảm bảo chất lượng sản phẩm. Tuy nhiên, để mở rộng phạm vi ứng dụng trong thực tiễn sản xuất, vẫn cần tiếp tục nghiên cứu một số vấn đề như: phát triển phương pháp đo độ dày cho vật liệu nhiều lớp, và hiệu chỉnh ảnh hưởng của hình học mẫu phức tạp dạng ống tròn, mặt cong hoặc bề mặt nghiêng.

| TẬP THỂ CÁN BỘ HƯỚNG DẪN (Ký tên, họ tên) Trần Thiện Thanh | NGHIÊN CỨU SINH (Ký tên, họ tên) Huỳnh Đình Chương |
| --- | --- |

XÁC NHẬN CỦA CƠ SỞ ĐÀO TẠO

HIỆU TRƯỞNG

Trần Lê Quan

THESIS INFORMATION

Thesis title: Research and development of a thickness measurement method for material plates based on gamma-ray transmission technique

Speciality: Atomic and Nuclear Physics

Code: 62440501

Name of PhD Student: Huynh Dinh Chuong

Academic year: 2016

Supervisor: Assoc. Prof. Dr. Trần Thiện Thanh

At: VNUHCM - University of Science

1. SUMMARY:

The thesis focuses on the development of a gamma-ray transmission (GT) measurement system using a 137Cs radioactive source and a NaI(Tl) detector for accurate determination of thickness in homogeneous material plates. The MCNP code (version 6.1) was used to simulate the GT measurements and to generate a comprehensive dataset for system calibration. To ensure high accuracy in the simulation results, the detector configuration were precisely modeled based on specifications obtained from a low-energy photon beam scanning method. The simulation results show strong agreement with experimental results; in particular, the relative deviation (RD) between simulated and experimental full-energy peak efficiencies remains below 3.5% across the photon energy range of 31–1408 keV, for standard source measurements at source-to-detector distances of 0 mm and 300 mm.

Based on simulations, the thesis established a comprehensive spectral dataset corresponding to a wide range of materials with effective atomic numbers from 3 to 83 and sample thicknesses between 0.1 mm and 70 mm. A quantity, referred to as the R ratio, was calculated by dividing the full-energy peak area obtained from measurements with the sample by the measurement without sample. The ln(R) values, derived from simulation data, ​​were used to construct an analytical calibration curve for thickness determination. The thickness of an actual sample can then be determined by interpolating the experimental ln(R) values into this calibration curve. The accuracy of the proposed method was validated using data from 162 experimental measurements on samples of graphite, aluminum, C45 steel and copper. Results indicate that the average RD between the measured and actual thicknesses is 0.52%, with the maximum RD not exceeding 2.17%.

In addition, the thesis introduces a method for estimating the range of measurable thickness (RMT) corresponding to a specified desired accuracy (DA) in the GT technique. The results demonstrate that, for all cases in which the sample thickness falls within the estimated RMT, the resulting RD consistently remains below the predefined DA threshold.

2. NOVELTY OF THESIS:

- A low-energy photon beam scanning method is proposed to accurately determine important specifications of the NaI(Tl) detector, including the diameter and length of crystal, the distance from the window to the crystal, and the mass density of the reflector. These specifications are used to construct the simulation configuration, thereby enabling the generation of highly accurate simulation data.

- A fitting formula is introduced for the rapid and precise calculation of the buildup factor, applicable to materials with effective atomic numbers ranging from 3 to 83 and thicknesses up to 70 mm. This formula enables accurate assessment of the contribution of scattered gamma-rays in the GT technique.

- A semi-empirical method is proposed for determining the thickness of material plates using the obtained spectrum from the GT technique. In this method, the analytical calibration curve is derived entirely from Monte Carlo simulation data, eliminating the need for reference samples. This significantly reduces operating costs and enhances the flexibility of the system, making it especially suitable for measuring the thickness of a wide variety of materials in industrial environments.

- A method is developed to estimate the RMT corresponding to a user-defined DA in the GT technique. This method supports users in proactively selecting appropriate measurement parameters, optimizing the acquisition time, and ensuring the reliability of results in non-destructive testing applications.

3. APPLICATIONS/ APPLICABILITY/ PERSPECTIVE

The research results of the thesis can be directly applied to the thickness inspection of material plates on industrial production lines, contributing to quality control of product. However, to further broaden the applicability of the GT technique in diverse real-world manufacturing scenarios, additional studies are needed. In particular, future research should focus on developing thickness measurement techniques for multilayer materials, as well as addressing the influence of complex sample geometries such as cylindrical tubes, curved surfaces, and inclined planes which frequently arise in practical engineering and industrial applications.

| SUPERVISOR Tran Thien Thanh | PhD STUDENT Huynh Dinh Chuong |
| --- | --- |

CERTIFICATION

UNIVERSITY OF SCIENCE

PRESIDENT

Tran Le Quan